Numerical Prediction of Fatigue-Cycle Threshold for Delamination Onset in Composite Laminates Using LS-DYNA

Abstract

Delamination under cyclic loading is a dominant failure mechanism in laminated composites. Predicting the number of fatigue cycles to initiation of delamination growth (onset) is essential for design and life-management. This work develops an analysis tool that couples a finite-element model with a user-provided G-N relationship obtained from experiments to predict the fatigue-cycle threshold for crack-growth onset along a laminate interface. The model employs a cohesive-zone formulation to represent the interface traction–separation response and to compute the local strain-energy release rate components GI,GII at potential crack-front locations each cycle. For a given loading ratio R and maximum energy-release rate Gmax, the code interpolates the experimental G-N curve and returns the predicted cycles to fatigue delamination crack onset Nonset. We demonstrate the workflow on a Double Cantilever Beam (DCB) configuration and provide color-maps of G along the interface to identify the most critical regions. Model predictions are planned to be validated against independent fatigue DCB tests using the same material system and layup. The resulting tool supports parametric studies (load amplitude, R-ratio, mode mixity) and can be extended to mixed-mode criteria and different cohesive laws.

Keywords: composites, delamination, fatigue, G-N, cohesive zone, LS-DYNA, DCB

- Contents

1.	Introduction	6

2.	Background	7

2.1	Composite Laminates	7

2.2	Fracture modes in laminates and strain-energy release rate	8

2.3	Fatigue parameters and load cycle definitions	10

2.4	Mechanism of crack propagation in the interface due to fatigue loading	12

2.5	Static onset criterion and the G–N diagram	14

3.	Numerical Method	16

3.1	Modeling principle	16

3.2	Cohesive zone element: role and constitutive law	16

3.3	The numerical process	17

3.4	Computing G(t) per element	19

3.5	From G_max to N: the per-element fatigue map	19

4.	Bibliography	21

5.	Appendix A	26

A.1.	Geometric properties and test description for UD Size 1 – baseline	26

List of Tables

No table of figures entries found.

List of Figures

Figure 1: A cross-section of two layers of a laminated composite material	7

Figure 2: Illustration of the three basic fracture modes: Mode I (opening), Mode II (in-plane shear), and Mode III (out-of-plane shear).	8

Figure 3: Typical fatigue loading cycle	11

Figure 4: Schematic Interface Crack progression in a composite specimen undergoing fatigue cycles. I – Undamaged specimen containing an initial pre-manufactured crack of length a0. II –V – Damage development and fatigue crack onset due to fatigue loading.	13

Figure 5: A schematic G-N Graph.	15

# Introduction

Modern aerospace and automotive structures increasingly rely on laminated composites due to their high specific stiffness and strength, corrosion resistance, and design flexibility. Yet delamination - the separation of adjacent plies along their interface, which remains a governing damage mode, particularly under cyclic loading where crack initiation may occur well below the static onset level. Designing against delamination therefore requires not only static toughness data, but also an ability to predict the conditions and number of cycles that lead to the onset of interfacial crack growth.

A standard experimental approach characterizes fatigue behavior through G-N curves, which relate an applied (mode-specific or mixed-mode) energy-release rate amplitude to the number of cycles to onset of delamination growth. These curves are obtained experimentally, and form the empirical backbone used for life prediction. Numerical models are then used to evaluate local G under service loading and to interpret or generalize the test results to structures and load cases beyond the tested configurations, to predict fatigue life onset in the structure.

This project develops a simulation-based analysis workflow for evaluating delamination onset under cyclic loading in composite laminates by combining finite-element results with experimentally measured fatigue behavior.

Within this framework, delamination is represented using a cohesive interface formulation in LS-DYNA. The analysis extracts cycle-dependent interface quantities (tractions and separations) to evaluate the corresponding energy-release-rate components, and then uses experimentally obtained G–N curves to estimate the number of fatigue cycles to delamination onset at the most critical interface location.

The remainder of this report is organized as follows. Section 2 summarizes the scientific background required for the subsequent sections. Section 3 presents the numerical method and post-processing approach. Section 4 outlines example outputs and discusses sensitivity to loading parameters. Finally, Section 5 describes the planned validation approach and acceptance criteria.

# Background

This section summarizes the concepts needed to model fatigue‑driven delamination in laminates. We begin with composite laminate construction and failure modes, proceed to strain‑energy release rate definitions, and then describe fatigue parameters and the G-N framework used to define onset.

## Composite Laminates

Figure 1: A cross-section of two layers of a laminated composite material

matrix

Fibers

Interface

Composite laminates consist of stacked plies of stiff fibers in a matrix (as shown in Figure 1). Interfaces between plies may get deboned, leading to delamination, which is a primary damage mechanism in composite laminates service.

Figure 1 shows a simplified cross-section of a composite laminate with only two plies. For clarity, the fiber direction is shown identical in both plies; in practical laminates the fiber orientation typically varies from ply to ply (e.g., 0/±45/90) to tailor stiffness and strength. Although the matrix and the inter-ply region are made of the same resin, the interface is fiber-free and therefore commonly becomes the weakest plane where delamination is most likely to initiate.

## Fracture modes in laminates and strain-energy release rate

Interfacial cracks in laminated composites can develop and propagate under different loading configurations. These configurations are traditionally categorized into three fundamental fracture modes, which describe the relative deformation between the two crack faces. The modes are illustrated in Figure 2, and the terminology used throughout this report follows this standard classification.

- Mode I (opening mode) – the two crack surfaces separate in the direction normal to the interface.

- Mode II (sliding / in-plane shear mode) – the crack surfaces slide relative to one another in the plane of the interface but perpendicular to the crack front.

- Mode III (tearing / out-of-plane shear mode) – the crack surfaces shear relative to one another parallel to both the interface and the crack front.

Mode I and Mode II are typically the dominant modes in laminated composites, whereas Mode III is often negligible compared to the other two due to laminate geometry and loading constraints.

These mode descriptions provide the basis for defining the strain-energy release rate and its modal components, which quantify how much mechanical energy becomes available for crack growth under each loading type.

Figure 2: Illustration of the three basic fracture modes: Mode I (opening), Mode II (in-plane shear), and Mode III (out-of-plane shear).

Mode I - opening

Mode II - sliding

Mode III - tearing

The strain-energy release rate, denoted G, represents the amount of mechanical energy released by the structure per unit increase in crack surface area as the crack advances. For interfacial cracks in composite laminates, it is customary to decompose G into contributions from the individual modes:

Gtotal=GI+GII+GIII.

Each modal component corresponds to one of the fracture modes shown in Figure 2. The relative dominance of these components is often expressed in terms of mode mixity, which quantifies the proportion of shear-related energy release (GII,GIII) relative to opening (GI).

Crack propagation occurs when the available energy release rate reaches a material-dependent critical value. For pure modes, these critical fracture toughness values are denoted:

- GIc– critical energy release rate in Mode I,

- GIIc– critical energy release rate in Mode II,

- GIIIc– critical energy release rate in Mode III.

Thus, for example, a crack subjected primarily to opening deformation will propagate once

GI≥GIc.

Under mixed-mode loading, an effective critical toughness Gc(ψ) is evaluated using an appropriate mixed-mode fracture criterion, where ψ is a mode-mixity measure (e.g. ψ=tan⁡-1(GII/GI)). This mixed-mode formulation allows the model to capture realistic loading conditions where Mode I and Mode II interact.

This definition of G and its critical values forms the basis of the numerical method used later in the report to evaluate delamination growth in composite laminates.

## Fatigue parameters and load cycle definitions

Fatigue is the progressive accumulation of damage in a material subjected to repeated sub-critical loading. Each individual load cycle is far below the static failure level, yet over a sufficient number of cycles the material develops microscopic flaws that grow, coalesce, and eventually become a macroscopic crack. In delamination problems the relevant damage mechanism is the gradual loss of cohesion at an interface under repeated opening or sliding of the adjacent plies. Characterising fatigue therefore requires describing the load cycle itself — its amplitude, mean level, ratio between maximum and minimum, and frequency — because all of these influence how quickly damage accumulates.

Xmax

Xmin

A

T

Amplitude

Time

Typical fatigue loading cycles are shown in Figure 3. They can be described by the maximum and minimum values of a load-related quantity X - (stress σ, displacement δ, or energy-release rate G) with period T and frequency f=1/T. The amplitude is A=Xmax-Xmin (where X denotes the chosen quantity), and the load ratio is R=Xmin/Xmax. In delamination studies, it is common and clearer to define these in terms of G rather than σ, because crack onset and propagation is governed by energy-release rate values at the crack tip.

Figure 3: Typical fatigue loading cycle

## Mechanism of crack propagation in the interface due to fatigue loading

Fatigue damage at an interface between composite laminate plies develops gradually through repeated loading.  Figure 4 shows a schematic side view of a composite specimen, undergoing fatigue loading cycle. In Figure 4.I, the specimen is shown in undamaged state. The specimen contains an initial pre-manufactured crack of length a0, located between two "arms", which undergo a cyclic,  mode-I loading.  Figure 4.II shows the specimen following several load cycles. micro-cracks begin to nucleate ahead of the crack tip.
Initially, small micro-cracks nucleate ahead of the pre-existing crack tip. As cycling continues, (Figure 4.III), these cracks grow, coalesce. Continued cycling causes the leading cracks to coalesce into a larger damage zone (Figure 4.IV), and form a larger damage zone. Once the accumulated damage reaches a critical level (Figure 4.V), the main delamination front advances by a measurable increment Δa. The initial advance of the crack due to the cyclic loading is termed fatigue crack onset.

Figure 4: Schematic Interface Crack progression in a composite specimen undergoing fatigue cycles. I – Undamaged specimen containing an initial pre-manufactured crack of length a0.
II –V – Damage development and fatigue crack onset due to fatigue loading.

a0

II

V

Δa

IV

III

I

a1

From an engineering design perspective, it is crucial to predict whether an existing crack within a composite component will grow under a given cyclic loading scenario. The G-N diagram provides an experimentally calibrated link between loading level and cycles to onset; the next section presents the numerical method used to compute the relevant energy-release rate quantities along the interface and map them onto the G-N data.

## Static onset criterion and the G–N diagram

Onset is defined as the first detectable crack extension under monotonic (non-cyclic) loading, determined via load drop, compliance change, or microscopic observation. The corresponding fatigue onset, addressed in the next section, is the analogous event under cyclic loading and is what the present work predicts.

The energy release rate at the onset point is denoted as GC and it defines a critical toughness for the interface (mode-dependent). Under cyclic loading with ratio R, an experimental G-N relationship gives the number of cycles N to onset for a given applied maximum energy-release rate Gmax (often expressed as a fraction of the Mode I.II, or II onset toughness (GIc,GIIc,GIIIc respectivly) and for a given load ratio R and mode mixity.

As seen in Figure 5 the horizontal axis is the number of cycles to onset (typically plotted on a logarithmic scale). The vertical axis is the applied maximum energy-release rate, often normalized by the static (monotonic) critical energy-release rate Gc, and therefore regions below the curve are generally safe-the applied energy-release rate is insufficient to nucleate detectable crack growth-while regions above the curve lead to onset (propagate) the crack within N cycles.

.

Figure 5: A schematic G-N Graph.

No growth

Crack growth

GC/Gmax

N

A typical G–N curve is illustrated schematically in Figure 5. It is constructed from experiments as follows. For simplicity, the workflow is described here for mode-I crack propagation, but can be repeated for other modes of loading, as needed. First, a static (monotonic), Mode I DCB test is performed to determine the onset toughness. Next, several cyclic fatigue tests are performed at several fractions of GIc (such as 0.9, 0.8, 0.7…) at a fixed R-ratio. For each GIc ratio chosen, the number of cycles to delamination onset is measured and plotted. The final curve is obtained by fitting/interpolating a smooth trend through the discrete experimental points.

In the next section we present the numerical procedure used to evaluate the cycle-dependent energy-release rate G along the interface.

# Numerical Method

the LS-DYNA solver writes nodal displacements (nodout) and element stresses (elout); a Python post-processor reads these together with the experimental G–N curve - supplied as a separate LS-DYNA keyfile so that the same curve can be re-used across analyses of different parts made of the same material - reconstructs the traction–separation history of each cohesive element, integrates it to obtain G(t), and inverts the G–N curve to convert the peak value Gmax into a cycle count.

In this FEM simulation we make use of a “cohesive element”, which is a finite element that has an opening-displacement relation described using a traction-separation law. The full constitutive form is given in Section 3.2.

## Modeling principle

As shown in Figure 6, the geometry is represented as two solid bodies separated by a thin layer of cohesive elements. The two bodies - for a delamination problem the adjacent composite plies - carry the bulk stiffness and inertia of the part; the cohesive layer represents the adhesive-like medium where the crack can initiate and grow. When the two bodies open (Mode I) or slide (Mode II) relative to each other, the cohesive elements develop tractions that oppose the relative separation.

[Figure 6 — schematic placeholder. Two solid bodies separated by a thin layer of cohesive elements. Label the upper body, lower body, and the cohesive layer; show arrows for normal traction T_n and shear traction T_s; indicate the bottom-face nodes (n1..n4) and top-face nodes (n5..n8) of one representative cohesive element.]

Figure 6: Schematic of the finite elements model of the system.

## Cohesive zone element: role and constitutive law

A cohesive element relates interfacial tractions T={Tn, Ts} to the relative separations Δ={Δn, Δs} between the opposing faces of the interface with n designating normal/opening, and s designating shear/sliding. The traction-separation law is defined so that the area under the curve equals the mode-specific fracture energies:

|  | GI = 0ΔnmaxTn dΔn, GII = 0ΔsmaxTs dΔs | Eq. (1) |
| --- | --- | --- |

A common form is the bilinear traction–separation law, illustrated in Figure 7: the traction rises linearly to a peak Tmax at the damage-onset separation Δ0, then drops linearly to zero at the critical separation Δf, beyond which the element is fully decohered. The mode-specific fracture energy is the area under this curve, G = ½TmaxΔf. Two material parameters control the law per mode - the peak strength (T_n,max for opening, Ts,max  for sliding) and the critical fracture energy (GIc, GIIc). Under mixed-mode loading an effective critical energy Gc(ψ) is obtained from a mode-mixity rule, with mode-mixity angle ψ = tan-1GIIGI.

[Figure 7 - bilinear traction–separation law. Plot T (vertical axis) versus Δ (horizontal axis). Linear rise from the origin to the peak point (Δ₀, T_max), then linear softening down to (Δ_f, 0); shade the area under the curve and label it G (= ½ T_max Δ_f). Mark Δ₀ and Δ_f on the horizontal axis. Caption note: the same bilinear shape is used for Mode I (T = T_n vs Δ_n) and Mode II (T = T_s vs Δ_s); the mode index is omitted for clarity.]

Figure 7: Bilinear traction–separation law used for the cohesive interface (Mode I and Mode II).

## The numerical process

The procedure (Figure 8) consists of the following steps:

Pre-run setup. The user prepares the LS-DYNA input deck - mesh, cohesive material card (peak strength and critical fracture energy per mode), boundary conditions and loads - and a separate keyfile containing the experimental G–N curve as a *DEFINE_CURVE_TITLE block titled “G-N”. Alternatively, the curve can be embedded directly in the main keyfile.

- The simulation is run in LS-DYNA, which writes node displacements (nodout) and element stresses (elout).

- The post-processor parses nodout and elout together with the LS-DYNA keyfile (and, if used, the separate G–N keyfile). A subset of cohesive elements can be flagged for analysis via *SET_SOLID blocks; on large models this keeps memory and run-time manageable.

- For each cohesive element in the analysis set, the per-time-step quantities below are computed:

  - Traction. The normal traction Tn is the stress component aligned with the face normal n  (chosen automatically among σxx, σyy, σzz by the axis n is closest to). The shear traction Ts is the magnitude of the two in-plane shear components consistent with that orientation.

  - Separation. Δ(t) is the average over the four cross-face node pairs (ni, ni+4), Δt= ¼ Σᵢ (utop,i - ubot,i), decomposed into Δn = Δ · n (Mode I) and Δt = Δ2- Δn2 (Mode II).

  - Energy-release rate. G(t) is obtained by integrating T over Δ in time; the trapezoidal scheme used is given in Section 3.4.

Steps 3a–3c are run for Mode I and Mode II independently, and the peak Gmax  = maxt G(t) is recorded per mode.

- Gmax is converted to a per-element cycle count N by inverting the experimental G-N curve, yielding the fatigue map N(e); see Section 3.5.

[Figure 8 — process flowchart placeholder. Render the Mermaid source below to a PNG and place it here. Mermaid source: flowchart TD;  A['LS-DYNA static-onset run'] arrow B['Outputs: nodout, elout'];  A arrow C['Keyfile (.k): geometry + G–N curve'];  B arrow D['Parse with LS_Post_data_reader'];  C arrow D;  D arrow E['For each cohesive element'];  E arrow F['Compute G_I(t), G_II(t), G_total(t)'];  F arrow G['Take G_max per mode'];  G arrow H['Fit log G = a + b log N from experimental G–N curve'];  H arrow I['Invert: N_I, N_II per element'];  I arrow J['N_critical = min(N_I, N_II)'];  J arrow K['Per-element fatigue map N(e)'];  K arrow L['Plotly preview'];  K arrow M['Export .scl for LS-PrePost']. (Replace 'arrow' with the standard Mermaid arrow when rendering.)

From a single static-onset LS-DYNA simulation, the program reconstructs G(t) for every cohesive element from nodout and elout, takes Gmax per mode, fits and inverts the experimental G–N curve (supplied as a separate keyfile or embedded), and produces the per-element fatigue map N(e).

## Computing G(t) per element

Given the traction and separation histories built in Section 3.3, the fracture-energy integrals (Eq. 1) are evaluated by the trapezoidal rule. Writing σi = T(ti) and δi = Δ(ti) at output time ti, each increment and the running integral are:

| Eq. (2) | ΔGi =12 (σi + σi-1) · ¦δi - δi-1¦ |  |
| --- | --- | --- |
| Eq. (3) | tk= i=1kΔGi, Gmax = maxt G(t) |  |
| Eq. (4) | GIt= 0tTndΔn, GIIt= 0tTsdΔt, Gtotal(t) = GI(t) + GII(t) |  |

One implementation note: no monotonicity is assumed. G(t) is tracked as a running integral, so the same code path also works for non-monotonic load histories. The shear traction in Eq. (4) is built from the two in-plane shear components consistent with the face normal n (e.g. σxy and σzx when n is closest to the x-axis), so the formulation is independent of the orientation of the cohesive layer in the global frame.

## From G_max to N: the per-element fatigue map

The (N, G) points of the embedded G–N curve are fitted by least squares in log–log space, log G= a + b⋅ log (N), and the fit is inverted per element:

| Eq. (5) | N = explog Gmax- ab |  |
| --- | --- | --- |

Eq. (5) is applied independently to Gmax,I and Gmax,II, giving NI and NII per element; the per-element life is then Ncritical = minNI, NII, the dominant mode setting the time of onset. The resulting field N(e) is the output of the analysis. It is rendered in two ways (Figure 9): an interactive 3-D preview inside the post-processor, and an LS-PrePost Script Language (.scl) export that reproduces the same fringe on the original LS-DYNA mesh.

[Figure 9 - placeholder. Per-element fatigue map N(e) for the DCB benchmark, log₁₀N colour scale. Lower values (red end) indicate elements predicted to reach onset first; higher values (blue end) are safer. Insert a screenshot of the Plotly preview from the post-processor or the LS-PrePost SCL fringe.]

# Bibliography

| [1] | A. Forghani, N. Zobeiry, A. Poursartip and R. Vaziri, "A structural modelling framework for prediction of damage development and failure of composite laminates," Journal of Composite Materials, vol. 47, no. 20-21, p. 2553 – 2573, 2013. |
| --- | --- |
| [2] | N. Zobeiry, Extracting the strain-softening response of composites using full-field displacement measurement, University of British Columbia, 2010. |
| [3] | X. Xu, M. R. Wisnom, Y. Mahadik and S. R. Hallett, "Scaling of fracture response in Over-height Compact Tension tests," Composites Part A: Applied Science and Manufacturing, vol. 69, pp. 40-48, 2014. |
| [4] | O. J. Nixon-Pearson, S. R. Hallett, P. W. Harper and L. F. Kawashita, "Damage development in open-hole composite specimens in fatigue. Part 2: Numerical modelling," Composite Structures, vol. 106, pp. 890-898, 2013. |
| [5] | K. Hoos, E. V. Iarve, M. Braginsky, E. Zhou and D. H. Mollenhauer, "Static strength prediction in laminated composites by using discrete damage modeling," Journal of Composite Materials, vol. 51, no. 10, pp. 1473-1498, 2017. |
| [6] | H. Bao and G. Liu, "Progressive failure analysis on scaled open-hole tensile composite laminates," Composite Structures, pp. 890-898, 2013. |
| [7] | P. W. Harper, L. Sun and S. R. Hallett, "A study on the influence of cohesive zone interface element strength parameters on mixed mode behavior," Composites Part A: Applied Science and Manufacturing, vol. 43, no. 4, p. 722 – 734, 2012. |
| [8] | N. Zobeiry, R. Vaziri and A. Poursartip, "Characterization of strain-softening behavior and failure mechanisms of composites under tension and compression," Composites Part A: Applied Science and Manufacturing, vol. 68, pp. 29-41, 2015. |
| [9] | X. Xu, M. R. Wisnom and S. R. Hallett, "Deducing the R-curve for trans-laminar fracture from a virtual Over-height Compact Tension (OCT) test," Composites Part A: Applied Science and Manufacturing, vol. 118, pp. 162-170, 2019. |
| [10] | A. Matzenmiller, J. Lubliner and R. L. Taylor, "A constitutive model for anisotropic damage in fiber-composites," Mechanics of Materials, vol. 20, pp. 125-152, 1995. |
| [11] | X. Li, S. R. Hallett and M. R. Wisnom, "Modelling the effect of gaps and overlaps in automated fibre placement (AFP)-manufactured laminates," vol. 22, no. 2, pp. 115-129, 2015. |
| [12] | X. Li, S. R. Hallett, M. R. Wisnom, N. Zobeiry, R. Vaziri and A. Poursartip, "Experimental study of damage propagation in Over-height Compact Tension tests," Composites Part A: Applied Science and Manufacturing, vol. 40, no. 12, pp. 1891-1899, 2009. |
| [13] | M. J. Laffan, S. T. Pinho, P. Robinson and A. J. McMillan, "Translaminar fracture toughness testing of composites: A review," Polymer Testing, vol. 31, no. 3, pp. 481-489, 2012. |
| [14] | I. Kongshavn and A. Poursartip, "Experimental investigation of a strain-softening approach to predicting failure in notched fibre-reinforced composite laminates," Composites Science and Technology, vol. 59, no. 1, pp. 29-40, 1999. |
| [15] | Livermore Software Technology Corporation, LS-DYNA R9.3.1, Livermore Software Technology Corporation, 2019. |
| [16] | Livermore Software Technology Corporation, LS-DYNA® KEYWORD USER'S MANUAL, vol. Volume II, 2016. |
| [17] | M. Shahbazi and R. Vaziri, "Simulation of the open-hole tensile response of composite Laminates Using a combines discrete and continuum damage approaches," in Proceedings of the 21st International Conference on Composite Materials, ICCM 2017, 2017. |
| [18] | X. Li, S. R. Hallett and M. R. Wisnom, "Numerical investigation of progressive damage and the effect of layup in overheight compact tension tests," Composites Part A: Applied Science and Manufacturing, vol. 43, pp. 2137-2150, 2012. |
| [19] | S. R. Hallett, B. G. Green, W. G. Jiang and M. R. Wisnom, "An experimental and numerical investigation into the damage mechanisms in notched composites," Composites Part A: Applied Science and Manufacturing, vol. 40, pp. 613-624, 2009. |
| [20] | S. Gerlach, M. Fiolka and A. Matzenmiller, "Modelling and analysis of adhesively bonded joints with interface elements for crash analysis," in LS-DYNA FORUM, 2015. |
| [21] | P. Maimí, P. P. Camanho, J. A. Mayugo and C. G. Dávila, "A continuum damage model for composite laminates: Part II - Computational implementation and validation," Mechanics of Materials, vol. 39, no. 10, pp. 909-919, 2007. |
| [22] | P. Maimí, P. P. Camanho, J. A. Mayugo and C. G. Dávila, "A continuum damage model for composite laminates: Part I - Constitutive model," Mechanics of Materials, vol. 39, no. 10, pp. 897-908, 2007. |
| [23] | X. Xu, M. R. Wisnom, X. Li and S. R. Hallett, "A numerical investigation into size effects in centre-notched quasi-isotropic carbon/epoxy laminates," Composites Science and Technology, vol. 111, pp. 32-39, 2015. |
| [24] | Hexcel, "HexPly® M21 Product Data Sheet," 2020. [Online]. Available: https://www.hexcel.com/user_area/content_media/raw/HexPly_M21_global_DataSheet.pdf. [Accessed 01 01 2024]. |
| [25] | Hexcel, "HexTow® AS4C Carbon Fiber Datasheet (Aerospace)," 2023. [Online]. Available: https://www.hexcel.com/user_area/content_media/raw/AS4C_Aerospace_HexTow_DataSheet1.pdf. [Accessed 25 01 2024]. |
| [26] | Hexcel, "HexTow® IMA Carbon Fiber Datasheet," 2023. [Online]. Available: https://www.hexcel.com/user_area/content_media/raw/IMA_HexTow_DataSheet.pdf. [Accessed 25 01 2024]. |
| [27] | O. Shor, Hexply M21 UD and twill weave AFRL in plane characterization summary, DM 38554939, 2024. |
| [28] | P. A. Kongshavn I, "Experimental investigation of a strain-softening approach to predicting failure in notched fibre-reinforced composite laminates," Composites Science and Technology, vol. 59, no. 1, pp. 29-40, 1999. |
| [29] | V. R. P. A. Zobeiry N, "Characterization of strain-softening behavior and failure mechanisms of composites under tension and compression," Composites Part A: Applied Science and Manufacturing, vol. 68, pp. 29-41, 2015. |

# Appendix A

## Geometric properties and test description for UD Size 1 – baseline

Table A1 –geometric properties and test description for UD Size 1 – baseline Layup 1aQI-stacked.

UD Size 1 – baseline Layup 1aQI-stacked. test description; anotchtot (mm); t (mm); W (mm); specimen. semi-complete test - loaded until final failure, but test was unintentionally interrupted; 59.07; 6.05; 1; 106.13; 1; U-S1-L1a-EE1. 6.01; 2; 106.15; 2. 5.99; 3; 106.13; 3. 6.02; avg; 106.14; avg. complete test - loaded until final failure; 59.02; 6.09; 1; 106.15; 1; U-S1-L1a-EE2. 6.06; 2; 106.16; 2. 6.00; 3; 106.15; 3. 6.05; avg; 106.15; avg. complete test - loaded until final failure; 59.07; 6.01; 1; 106.32; 1; U-S1-L1a-EE3. 6.02; 2; 106.35; 2. 6.05; 3; 106.44; 3. 6.03; avg; 106.37; avg. interrupted test – loaded until first (small) drop; 59.01; 6.07; 1; 106.33; 1; U-S1-L1a-EE4. 6.05; 2; 106.34; 2. 6.03; 3; 106.32; 3. 6.05; avg; 106.33; avg. interrupted test – according to first high AE signal; 59.07; 6.04; 1; 106.15; 1; U-S1-L1a-FF1. 6.02; 2; 106.12; 2. 6.02; 3; 106.10; 3. 6.03; avg; 106.12; avg. interrupted test – according to first low AE signal; 59.06; 6.07; 1; 106.15; 1; U-S1-L1a-FF2. 6.04; 2; 106.15; 2. 6.04; 3; 106.17; 3. 6.05; avg; 106.16; avg. compliance calibration; 59.08; 6.05; 1; 106.35; 1; U-S1-L1a-FF3. 6.05; 2; 106.39; 2. 6.05; 3; 106.44; 3. 6.05; avg; 106.39; avg.